## Slide 1: 3D Printer Training
22-Sep-2016

## Slide 2: 3D Printers in the Design Studio
uPrint and Cube
  Initial prototypes
  Low resolution
  Large parts
Form2
  Later prints
  Higher resolution
  Smaller parts
  More detail
Set up time in the lab to set up the print AND to remove the parts
  uPrint and Form2 can be run overnight

## Slide 3: Split into 2 groups:
MB64
uPrint
Form2
MB78
Cube
Demo

## Slide 4: uPrint - software
Detect -> select printer
Add .stl file
Ensure units are correct
Process the part
  Part layers shown
  Support shown in purple
Part orientation:
  Inspect tray and optimize placement of parts
  Don’t print over gouges
  Print tall to conserve space on build tray
Add to pack
  Record how much time and material is being used
  Can save .cmb job file

## Slide 5: uPrint - printer
Use heat resistant gloves
Empty garbage bin inside
Insert tray, lock in place, engage blue clips
Change material (if necessary) via cartridges located at the bottom
Push the ‘start model’ button on the side
Removing parts:
  Use heat resistant gloves to remove the tray
  Use cut resistant gloves and scraper to remove parts from plate
  Use pliers to remove support material
  Can use water solution bath to remove excess support material (~10 hour soak)
    Put the part in the bath and change the sign to indicate bath to be turned on

## Slide 6: Form2
Ask Arushri to train a group member before using the printer
Use Preform software
  Upload part .stl file
  Select Form2 printer
  Select resin (Clear or Flexible)
  Orient on a slant
  Add supports
  Send to printer
Ensure the build platform is clean
  Alcohol on black part
  No alcohol on metal
Remove particles inside build tray
Follow instructions on printer screen
  Level printer
Start print
  Can leave overnight

## Slide 7: Form2
Remove part from build platform using spatula
Clean build platform
Soak parts in alcohol for 15 minutes
Blow dry
Post-processing
  Drill holes
  Tap hole
Let cure in sunlight